| Operations/Work/Job Activity covered by this assessment: Removal of Old Coating |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- |
| Required Personal Protective Equipment (PPE) : Safety glasses must be worn at times.; Long and loose hair must be contained.. Appropriate footwear with substantial uppers must be worn.; Close fitting/protective clothing to cover arms and legs must be worn.. Respiratory protection devices required.; Oil free leather gloves and spats must be worn.. Hearing protection must be used when using this machine.. |
| Loading & Unloading Check: - Ensure no slip/trip is present in work pass and walk ways. - Ensure that work area is clean and clear of grease, oil and any flammable materials. - Refer Work Instructions PSP/WI/14 while handling. |  |  |  |  |  |
| Operations Procedure: - To remove the old coating by means of Grit Blasting to achieve a clean parent metal substrate for further processing of coating. - De-grease the component to ensure a clean surface. Pre-inspect the component and note dimension of in the pre-inspection report. - Look for defects like pin holes, dents etc. if any, report to the Quality inspector. - Grit blast the coating area with appropriate grit size and pressure (application based). - Polish the component to observe any deformity on the surface. - Check the actual dimension after polishing and record it. - Repair the defects with the help of welding/buffing/cut on a lathe, grinding etc. to make the component fit for coating. |  |  |  |  |  |
| Assessor : |  | Signature: |  | Date: |  |
| Approved: |  | Signature: |  | Date: |  |