| Operations/Work/Job Activity covered by this assessment: Blasting |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- |
| Required Personal Protective Equipment (PPE) : Safety glasses must be worn at times.; Long and loose hair must be contained.. Appropriate footwear with substantial uppers must be worn.; Close fitting/protective clothing to cover arms and legs must be worn.. Respiratory protection devices required.; Oil free leather gloves and spats must be worn.. Hearing protection must be used when using this machine.. |
| Note: For Stainless Steel Components always use Virgin Aluminum Oxide Grit. Operation Procedure: # Check Job Card , Photographs , Customer name JC no. & PIR no. matches the job. Check if job hardness and MOC mentioned on PR. If not get it checked and updated from QC. # Set the blast parameters and select grit as per format no QF/QA/27 to achieve desired Ra. Use Virgin Aluminum Oxide Grit for job if mentioned on PIR . # Use go/no gauge on nozzle to check fitness of use. Replace nozzle if needed. # Moisture presence not desirable in blasting. Follow procedure QF/QMS/02/29 to check. Contact maintenance/ Production supervisor if found. # Correctly identify coated and non-coated areas and check masking integrity. Check Drawing & Sketch to ensure Coating and non-coating area, Contact QC/Masking dept. as and when if required. # Visually inspect the component as per VT procedure before and after blasting for check any deformities like dents, burrs etc. # While blasting Hold the job in proper fixture and handle it carefully. # Use 750 -800 angles and maintain 6” to 12” distance from the job to get desired surface roughness. # Do not over blast the surface by doing multiple passes and setting of wrong blast angle and pressure, as this will cause entrapping of the grit on blasted surface. # Make sure that the whole surface area of the component is blasted and no area is left. # Visually inspect the job after blasting and ensure that there is no defect. # If a micro pin hole is observed or oil residue from a pin hole / threaded portion, a burner or blower is used to remove the oil traces. # If required re-blast the affected area. # Blow air over the component after blasting to remove dust. # After final blasting, make sure the surface is uniformly blasted. Compare blasted surface with grit comparator and measure with test-ex tape where necessary to check conformance. # Fill the Job Card mentioning the date, grit & pressure for blasting and name of the blasting operator. # Get it approved from the Quality Inspector/QA/Spray Operator. # Operator to Ensure that coating is applied within 2 hours of completion of grit blasting to avoid surface contamination or oxidation. # Ask spray operator/ planner for the next jobs to be taken for blasting. Maintain backlog of “ready to spray jobs” for all spray stations to avoid downtime in spraying. |  |  |  |  |  |
| Assessor : | Prassana Wadkar | Signature: | PSW | Date: | 08.02.2026 |
| Approved: | Haarsh Doshi | Signature: | HDD | Date: | 08.02.2026 |