| Operations/Work/Job Activity covered by this assessment: Twin wire Arc Spray (TWAS) |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- |
| Required Personal Protective Equipment (PPE) : Safety glasses must be worn at times.; Long and loose hair must be contained.. Appropriate footwear with substantial uppers must be worn.; Close fitting/protective clothing to cover arms and legs must be worn.. Respiratory protection devices required.; Oil free leather gloves and spats must be worn.. Hearing protection must be used when using this machine.. |
| Loading & Unloading Check: - Ensure no slip/trip is present in work pass and walk ways. - Ensure that work area is clean and clear of grease, oil and any flammable materials. - Refer Work Instructions PSP/WI/14 while handling. |  |  |  |  |  |
| Operations Procedure: # Refer Pre-Inspection Work Instructions PSP/WI/12 to pre-inspect the Component. # Refer Final Blasting Work Instructions PSP/WI/04 for preparing surface. The surface preparation will be as per Sa3 specs. # Mask with High Temperature Adhesive Tape/Metal Shim/ to protect unwanted area from over spraying during TWAS spray coating. # Load the Component in the acoustic room and clamp it thoroughly on the chuck with proper packing to prevent clamping marks on the Component. # Start Exhaust Fans before starting the TWAS Control Unit. # Open valve of AIR and set the pressure according to the parameter mentioned in the Technical Bulletin. # Start the TWAS control unit with “On/OFF” switch. # Select the required Wire w.r.t the Job Card. # Measure the wire feed rate and Air pressure as per parameter, and set the Amperes and volts accordingly. # Set the job speed and Robot program speed, refer Job Card or instructions will be given by Supervisor/WM. # Closed the Acoustic Door and Wait for signal before igniting the Torch. # After ignition recheck the Amperes and Volt values and reset if required as per the desired parameter. # Intermediate dimension should be checked to control dimension as per job card.C # Check the dimension to get the desired thickness of the coating mentioned in the job card. # After completion of spraying of the component # Cool the job gradually and recheck the dimension. # Fill up the Job Card as per the data and Tag it. |  |  |  |  |  |
| Shutdown : # Shut the Switch and bring the Robot to its home position. # Cool the job gradually and recheck the dimension. Fill up the Job Card as per the data and Tag it. # Refer to Final Inspection Work Instruction PSP/WI/10 and get the approval Supervisor. |  |  |  |  |  |
| Assessor : |  | Signature: |  | Date: |  |
| Approved: |  | Signature: |  | Date: |  |