| Operations/Work/Job Activity covered by this assessment: Grinding Operation |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- |
| Required Personal Protective Equipment (PPE) : Safety glasses must be worn at times.; Long and loose hair must be contained.. Appropriate footwear with substantial uppers must be worn.; Close fitting/protective clothing to cover arms and legs must be worn.. Respiratory protection devices required.; Oil free leather gloves and spats must be worn.. Hearing protection must be used when using this machine.. |
| Loading & Unloading Check: - Ensure no slip/trip is present in work pass and walk ways. - Ensure that work area is clean and clear of grease, oil and any flammable materials. - Refer Work Instructions PSP/WI/14 while handling. |  |  |  |  |  |
| Operations Procedure: # Select the grinding wheel required as per the recommendation given by the Supervisor/Production Engineer/Works manager. # If component is coated with a hard material i.e. tungsten carbide, ceramic etc use a Diamond wheel and in other cases use a Silicon Carbide wheel/Aluminum Oxide wheel. # Refer the respective job card/ drg. of the component. # Mount the component between centers on the machine. # Check for run out maximum permissible limit is 0.02 microns or as per customers drg. # Set the Job Speed and feed speed. The depth of cut should not be more than 0.01mm for harder materials like Tungsten Carbide, Ceramic. Etc. and same should be 0.025mm for softer materials. # Intermediate dimension should be check as per the finish dimension in job card. # The operator/ quality inspector should record the dimension and surface roughness in the job card. # Remove the component from the Grinding machine in properly packed condition to avoid damages during unloading. # The component shall be properly packed with foam sheet and cotton tape / thermocol packing and will be kept at the dispatch section with yellow tagged for traceability. |  |  |  |  |  |
| Assessor : |  | Signature: |  | Date: |  |
| Approved: |  | Signature: |  | Date: |  |