| Operations/Work/Job Activity covered by this assessment: Cleaning Of components |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- |
| Required Personal Protective Equipment (PPE) : Safety glasses must be worn at times.; Long and loose hair must be contained.. Appropriate footwear with substantial uppers must be worn.; Close fitting/protective clothing to cover arms and legs must be worn.. Respiratory protection devices required.; Oil free leather gloves and spats must be worn.. Hearing protection must be used when using this machine.. |
| Operations Procedure: - Purpose of Cleaning is to ensure a clean and defect free surface. To proceed with the coating process. - Ensure that work area is clean and clear of grease, oil and any flammable materials. - Remove excess grease/oil by means cotton rags soaked in kerosene and wipe the component thoroughly. - Use only Acetone for aviation components which are made of Titanium and other parts with Trichloroethylene or as per instruction given by the Supervisor/ Works Manager. - Wipe the component thoroughly and rigorously. - For smaller components immerse them in the container with respected solution. - In case excess oil is found on the component’s coating surface use a burner to heat and remove the excess oil. - In case any burr, sharp edges or rusting is observed on the component use emery paper or pneumatic tools to remove deformities to ensure a smooth and a clean surface. |  |  |  |  |  |
| Assessor : |  | Signature: |  | Date: |  |
| Approved: |  | Signature: |  | Date: |  |