| Operations/Work/Job Activity covered by this assessment: Contact Plate |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- |
| Required Personal Protective Equipment (PPE) : Safety glasses must be worn at times.; Long and loose hair must be contained.. Appropriate footwear with substantial uppers must be worn.; Close fitting/protective clothing to cover arms and legs must be worn.. Respiratory protection devices required.; Oil free leather gloves and spats must be worn.. Hearing protection must be used when using this machine.. |
| Loading & Unloading Check: - Ensure no slip/trip is present in work pass and walk ways. - Ensure that work area is clean and clear of grease, oil and any flammable materials. - Refer Work Instructions PSP/WI/14 while handling of Contact Plate. |  |  |  |  |  |
| Operations Procedure: # Refer Pre-Inspection Work Instructions PSP/WI/03 to pre-inspect the Contact Plate. # If damaged is found on the coating surface, inform Gemsons Precision Engineering (P) Ltd. (GPEPL) by email with photograph and get their approval. # Repair to be carried w.r.t. (GPEPL) procedure. # Mark the area with the stencil w.r.t. drawing. # Mask with High Temperature Adhesive Tape/Metal Shim/Insulation tape to protect unwanted area from blasting and TWAC coating of Copper. # Ensure the Compressed Air is clean & free from water residues. # Refer Final Blasting Work Instructions PSP/WI/04 for preparing surface. The surface preparation will be as per Sa3 specs. # Use virgin 24mesh Al2O3 grit for blasting. Maintain Air pressure to blast at 3.5bar with 6mm bore nozzle and keeping 200 ±50mm standoff distances. # If any pinholes/micro pinholes are observed convey to supervisor for approval. # Maintain 5 to 8 Ra microns surface roughness during blasting and check visually. # Load the Contact Plate in the acoustic room and clamp it thoroughly on the fixture to prevent clamping marks on the Contact Plate. # Start Exhaust Fans before starting the TWAC Control Unit. # Open valve of AIr and set the pressure according to the parameter mentioned in the Technical Bulletin. # Start the TWAC control unit and set Amps and Voltas desired in the parameter. # Closed the Acoustic Door and Wait for signal before igniting the TWAC Torch. # Press the start button to ignite the TWAC Torch and set the Amps by turning the Air Flow valve to get the desire Amps 0f 125 to 150 Amps. # Start the Robot for evenly spraying of Contact Plate. # Repeat the Cycle two times to achieve the thickness of 60 to 90microns. # Reverse the Contact Plate to spray the sides and repeat Step 16 to 18. |  |  |  |  |  |
| Shutdown : # Turn off the valve to Shut down the TWAC flame and bring the robot to its home position. # Inspection: # Check the dimension to get the 60+20µm thickness of the coating. # Brush the coated area with Stainless steel wire brush to remove loose particles from the coated surface. # Refer to Final Inspection Work Instruction PSP/WI/10 and get the approval of GPEPL Representative. |  |  |  |  |  |
| Assessor : | Prasanna Wadkar | Signature: |  | Date: | 6/4/15 |
| Approved: | Dhimant Doshi | Signature: |  | Date: | 8/4/15 |