| Operations/Work/Job Activity covered by this assessment: Visual Inspection |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- |
| Required Personal Protective Equipment (PPE) : Safety glasses must be worn at times.; Long and loose hair must be contained.. Appropriate footwear with substantial uppers must be worn.; Close fitting/protective clothing to cover arms and legs must be worn.. Respiratory protection devices required.; Oil free leather gloves and spats must be worn.. Hearing protection must be used when using this machine.. |
| Loading & Unloading Check: - Ensure no slip/trip is present in work pass and walk ways. - Ensure that work area is clean and clear of grease, oil and any flammable materials. - Refer Work Instructions PSP/WI/14 while handling. |  |  |  |  |  |
| Operations Procedure: Visual inspection qualification: - - Only those personnel, Certified NDT level II or higher is qualified. - It shall perform when access is sufficient to place the eye within 24” of the surface and angle not less than 30° to the surface to be examined - Minimum light level shall be at least 750 to 1000 lux. - Artificial light can be used such as flashlight, drop light or ant other similar form of light to maintained minimum light level. - Magnifying lens can be used. # Scope: To check whether the coating and finished product as per customer requirements. # Take out print of FIR (Final-Inspection Report) format from software. # FIR indicates the Customer Name, Part Name, Qty etc… # Carry out Visual Inspection to check scratch, dents, pinholes, coating discontinuities etc., # Compare the component with Pre-inspection Report/ Drawing given by the Customer. # Record components details like, punch no and mention any remark/observation in the remark cells. # If discontinuities are found contact your Production Engineer/ Works Manager, and get clearance from the them # After getting the approval from the Production Engineer/ Works Manager, perform final inspection procedure. |  |  |  |  |  |
| Assessor : |  | Signature: |  | Date: |  |
| Approved: |  | Signature: |  | Date: |  |