Operations/Work/Job Activity covered by this assessment: Mounting Machine

Required Personal Protective Equipment (PPE) : Safety glasses must be worn at times.; Long and loose hair must be contained.. Appropriate footwear with substantial uppers must be worn.; Close fitting/protective clothing to cover arms and legs must be worn.. Respiratory protection devices required.; Oil free leather gloves and spats must be worn.. Hearing protection must be used when using this machine..

A B D C I A B D C I - Switch ON the power (A) - Check the waterline to ensure constant flow of water and lock the same. (B) - By operating the right hand side lever (C) move the spindle UP and open the lid in the mounting machine (D) - Apply the WD 40 spray(aerosol) on the inner surface of chamber and on top of the spindle (E) and on the inner surface of the top cover (F) F E H G F E H G - Weigh 18.5 gms of phenolic powder for mounting and keep it on a butter paper (G) - Keep the specimen on top of the spindle as shown (H) and lower the spindle by unlocking the knob on the right hand side (I) - Pour the powder in the chamber at centre of the hole very slowly. - Place the lid on the chamber and rotate it clockwise. M K L J N M K L J N - After tightening the lid from the top and just release a little by rotating anti-clockwise. - Lock the knob (I) on the right hand side. - Switch `ON’ the Mains situated on the backside of the machine (J) - Switch `ON’ Red power button (K) on the front right hand corner - When the display shows `Cycle complete’, switch on `Cycle heating’ (L) - Keep applying pressure through Right hand side lever (C) by pressing downwards continuously till the pressure reaches 2000 psi (M) and the temp reaches 1600 C. Maintain the pressure. - At 160OC temp and 2000 psi, the heating is stopped and the cooling process begins (N) - Switch on the water flow to the mould by opening the valve in the pipeline (B). - When the temperature of the mould reaches room temp, release the knob (I) and remove the lid (E) by rotating anticlockwise - Lock the Knob (I) and using the right hand side lever ©, raise the spindle up and remove the specimen.