Operations/Work/Job Activity covered by this assessment: Grinding Machine

Required Personal Protective Equipment (PPE) : Safety glasses must be worn at times.; Long and loose hair must be contained.. Appropriate footwear with substantial uppers must be worn.; Close fitting/protective clothing to cover arms and legs must be worn.. Respiratory protection devices required.; Oil free leather gloves and spats must be worn.. Hearing protection must be used when using this machine..

- After releasing the mounted specimen from Bain-Mount machine, clean the same with soap solution and the with running water. - Dry the specimen with good quality filter paper - With suitable engraver, put the specimen details on the backside of the mount so that it is parallel to the length of the specimen mounted. - Open the front cover and ensure that the Emery paper with Grit 80 is held firmly between the two rollers in the equipment - Close the front cover and switch ON the grinding machine. - Wear the proper fitting gloves on your hand. - When the emery starts rotating, hold the specimen as shown and start pressing against the rolling emery paper. - After few seconds viz., 20-30 secs, immerse the specimen in cold water or coolant kept in a beaker nearby and then remove the water on the specimen by drying with filter paper. - Repeat the process detailed in S.No. - The grinding process is over once the grinding lines are parallel and uniform over the entire length of the specimen