| Operations/Work/Job Activity covered by this assessment: Blasting and Ultrasonic cleaning (Sample) |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- |
| Required Personal Protective Equipment (PPE) : Safety glasses must be worn at times.; Long and loose hair must be scontained.. Appropriate footwear with substantial uppers must be worn.; Close fitting/protective clothing to cover arms and legs must be worn.. Respiratory protection devices required.; Oil free leather gloves and spats must be worn.. Hearing protection must be used when using this machine.. |
| Note : Always use clean transparent plastic gloves while handling the samples for blasting and ultrasonic cleaning. Operational Procedure: # Purpose of blasting is to clean and remove oxide layer from the surface. # Check the Work instructions from Supervisor. # Visually inspect the sample to check any deformities like dents, burrs etc. # Mask the job if required as per instructions given by the supervisor. # Hold sample in a suitable fixture and handle it carefully [Fig 1]. Fig 1. # Place the fixture horizontally on the metal frame in the blasting area. # Fill the grit tank with 80 grit Alumina powder. Use the Virgin Aluminum Oxide Grit always [Fig 2 –A] # Set the air pressure to 6.5 bar for getting the proper surface roughness. # [Fig 2 –B] A B Fig 2. # Wear a proper mask and blasting helmet before starting the blasting operation. [Fig 3]. # Use the 6 mm Nozzle for grit blasting operation. Use go no gauge on nozzle to check fitness of use. Replace nozzle if needed. # Blast the surface at 450 angles and maintain 6” to 8” distance from the job to get desired surface roughness. [Fig 4]. Fig 4. Fig 3. # Do not over blast the surface, as this will cause entrapping of the grit on blasted surface. # Make sure that the whole surface area of the sample is blasted and no area is left (as per Sa3). # Visually inspect the sample after blasting and ensure that there is no defect. # If the defect is not acceptable, change the sample with a new one. # Blow air over the component after blasting to remove dust. # After final blasting, make sure the surface is uniformly blasted. # Fill the Data Card mentioning the date, grit & pressure for blasting and name of the blasting operator. # Get it approved from the Supervisor. # After blasting, clean the surface of the material with soft bristle brush # [Fig 5]. Fig 5. # Clean the Ultrasonic bath with acetone and wipe out the inner chamber with fine tissue paper to remove dust and other particles. [Fig 6] # Fill the ultrasonic bath with approx. 250 ml of acetone. Fig 6. # Place the grit blasted samples inside the ultrasonic bath chamber using Tongs with blasted surface facing upwards. # Start the Ultrasonic bath for 10 minutes so that the blasted surface is cleared of fine grit particles. # Now the ultrasonic cleaned samples is ready for thermal spray coating process. |  |  |  |  |  |
| Assessor : |  | Signature: |  | Date: |  |
| Approved: |  | Signature: |  | Date: |  |