| Operations/Work/Job Activity covered by this assessment : Masking |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- |
| Work Instructions: # PIR or Job card must be collected from Planner / ISR (Inbound Sales representatives) before Masking. # Determine the area which is to be masked from the sketch or drawing present in PIR. # Select the masking tape/masking putty/shim/metal masking according to the process mentioned in the PIR/job card, i.e Green tape for PLASMA Process & Silver tape/metal masking/putty/shim for HVOF Process. # Clean the component with the help of acetone and make sure component is oil and Dust free after cleaning. # Begin masking the component by leaving atleast a gap of 2mm from coating area. # Mask two times at area which is adjacent to Coating area. # Make sure to apply proper pressure and eliminate all air pockets with the help of wooden stick. # Use insulation Tapes to cover the uncoated area of the Component and their by Complete the masking. # Fill the timesheet after complete masking. |  |  |  |  |  |
| Assessor : | Prasanna Wadkar | Signature: |  | Date: |  |
| Approved: | Haarsh Doshi | Signature: |  | Date: |  |