# PURPOSE # To outline the procedure for evaluating the quality and conformance of thermal spray coatings through standardized testing methods. # SCOPE # Applicable to all thermal spray-coated components and test coupons prepared in the facility. # REFERENCES # ASTM C633 – Adhesion Test # ASTM D7091 / ISO 2178 – Coating Thickness # ASTM E384 – Microhardness Test # ASTM E18 - Macrohardness Test # ASTM E2109 – Porosity Measurement # ASTM E1920 – Microstructure Evaluation # ASTM D4417 – Surface Roughness # ASTM D522 – Bend Test # RESPONSIBILITIES # Lab Technician: Perform and document all tests. # QC Engineer: Verify results and ensure compliance. # QA Head: Approve final reports. # EQUIPMENT REQUIRED # Surface Roughness Tester / Testex Tape # Coating Thickness Gauge (Eddy Current/Magnetic) # Pull-Off Adhesion Tester # Metallurgical Microscope # Microhardness Tester # Sample Preparation Tools (Cutter, Grinder, Polisher) # SAMPLE PREPARATION # Select coated test coupons or component sections. # Mount, grind, and polish to mirror finish. # Etch for microstructural evaluation if required. # TESTING PROCEDURE # 7.1 Coating Thickness # Standard: ASTM D7091 # Procedure: # Calibrate instrument. # Take 5 readings. # Record average, min, and max. # 7.2 Surface Roughness (Pre-Spray) # Standard: ASTM D4417 # Procedure: # Measure Ra or use Testex tape. # Record values before coating. # 7.3 Adhesion Test # Standard: ASTM C633 # Procedure: # Bond specimen with epoxy. # Cure and test pull-off strength. # Record force and failure mode. # 7.4 Microstructure Evaluation # Standard: ASTM E1920 # Procedure: # Use microscope to inspect bond line, Interfacial contamination, oxides. # Capture 20 images of each. # 7.5 Microhardness Test # Standard: ASTM E384 # Procedure: # Perform indentations across coating. # Take 5 readings. # Record average hardness. # 7.6 Bend Test # Standard: ASTM D522 # Procedure: # Perform Bend on 15/25mm dia rod and bend to 90/180 degree across coating # Check for crack. # No spalling/lifting acceptable, Coating spalling/lifting unacceptable. # 7.7 Porosity Measurement # Standard: ASTM E2109 # Procedure: # Use image analysis or manual grid. # Capture 20 images. # Report porosity % # REPORTING # Job/Coupon No.: _______________ # Coating Type: _______________ # Surface Roughness (Ra): ______ µm # Coating Thickness: Avg _____ µm (Min: ___, Max: ___) # Adhesion Strength: ______ MPa (Perform in another Lab) # Failure Mode: □ Cohesive □ Adhesive □ Substrate # Microstructure Observations: # Porosity: ______% # Hardness: ______ HV0.3/HRC/HR15N/HR15Y # Bend Test: Acceptable/Unacceptable # Final Status: □ Pass □ Fail # SAFETY PRECAUTIONS # Always wear lab PPE. # Use gloves when handling chemicals. # Operate machinery with guards in place. # DOCUMENT CONTROL # All test records and reports shall be maintained for a minimum of 5 years or as per quality system requirements.