# Operations/Work/Job Activity covered by this assessment: Sealant Application

Required Personal Protective Equipment (PPE) : Safety glasses must be worn at times.; Long and loose hair must be contained.. Appropriate footwear with substantial uppers must be worn.; Close fitting/protective clothing to cover arms and legs must be worn.. Respiratory protection devices required.; Oil free leather gloves and spats must be worn.. Hearing protection must be used when using this machine..

- Clean the surface thoroughly to remove dust. - Ensure thermal coating is fully cured and surface is clean and dry. - Apply scotch brite brush lightly on the coated surface to remove high points. - Ensure the sealant solution is properly mixed and loaded into the hopper. - Adjust air pressure within the range of 20 - 40 PSI. - Set the spray gun at a distance of 6 - 8 inches from the work surface. - Maintain a spray angle of approximately 90° to the surface. - Set the nozzle or air cap as per the surface type: - Vertical for cylindrical surfaces [Fig.1a] - Horizontal for rectangular surfaces [Fig.2a] Fig.1a Fig.2a Check nozzle position (Horizontal) - Perform a test spray on paper and confirm that the spray pattern is uniform without dripping. - Adjust screw to get proper spray pattern. - Begin sealant application within 30 minutes of preparing the solution. - Apply the sealant evenly, ensuring full coverage of the required area. - Cure for 8-12hours without touching the coated surface. Precautions : - Ensure the air pressure is stable during spraying. - Avoid excessive build-up of sealant in one area. - Clean spray gun thoroughly after use to prevent clogging. - Handle air equipment carefully to avoid accidents. - Make sure the Air in dry and no moisture.

Check nozzle position (Vertical)